## Slide 1: Composite Laser Ablation for Surface Preparation (CLASP) Making light work of composite bond prep
Presenter: Jimmy John
Laser Research Engineer | Laser Manufacturing Technology Development
AMTD Group| Structural Materials Division
University of Dayton Research Institute (UDRI)
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 2: Introduction – University or Dayton Research Institute (UDRI)
Established in 1956
Performs basic and applied research, engineering services, testing, & technology transition
Fully supported by external sponsors
Integral part of the University; reinforces UD’s mission
Over 800 research staff (250+ at WPAFB)
Among all colleges and universities:
  1st in the U.S. for materials R&D
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 3: Additive and Laser Manufacturing Technology Development
20+ person research group that can rapidly mobilize to deliver Additive Manufacturing, Laser Manufacturing, and Application-driven solutions.
  Laser Manufacturing Technology Development
    Ultra-fast laser system development
    Laser-material interaction
  Laser Powder Bed Fusion Additive Manufacturing
    Next Gen. Machine design and innovation
    Operates AFRL Novel AM Lab (RXCM)
    In-situ Laser Process Monitoring
    AM Materials Science and Testing
  Photopolymer AM
    Application driven
  Advanced Applications
    Rapid application development across all UDRI technologies
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 4: UDRI Ultrafast Laser Capabilities
20W Amplitude FS laser
  Mobile fiber launch
20W IPG FS laser
  On 5 axis Aerojet workstation
30W IPG Nanosecond (NS) laser
  Supports STT "Enterprise Product"
50W Amplitude FS laser
  With harmonic generator
100W Amplitude FS laser
  Hybrid LPBF
300W Amplitude FS
  In negotiation, ETA 2024
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 5: Composites Processing Case Study
  Composite bond preparation can be a complicated process depending on the application. Current methods of hand sanding (Sand-to-Black) have many challenges:
    Variable efficiency by operator
    Requires multiple steps to ensure preparation for bond is complete
    Manually intensive
    Time consuming
  A more efficient, quality replacement for manual sanding is desired.
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 6: What is CLASP?
  Composite Laser Ablation Surface Preparation
    CLASP is an ultrafast laser, surface preparation method
    Developed under AFRL ManTech Discovery Fund
    Goal is to streamline the PMC bond prep process
SAND TO BLACK
CLASP
Ronnie Gadola, 574th Composite Repair Flight sheet metal mechanic, sands an F-15 torque box assembly in a new sanding booth in Bldg. 169. U. S. Air Force photo by Ray Crayton Jr
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 7: Why Now? Why this Technology?
  Femtosecond lasers have scaled in power greatly over the past decade
    4W was state-of-the-art in 2011
    Today, commercial systems are available in 300W+
  Hollow core fibers are now commercially available, allowing ultrafast pulses at the fibers end
  Current commercial fiberoptic delivery technology is IR wavelength coated ONLY
    It is understood that other wavelengths may provide additional benefits (532nm, 355 nm)
    Ongoing studies with bench-top laser systems are quantifying benefits of lower wavelength to the process
  As the technology matures and market pull increases, better fibers will likely become available
    More wavelengths
    Higher average power
    Higher pulse energies
Photonics Tools Beam launching system
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 8: Long Pulse Laser (NS) vs Ultra Short Laser (FS)
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992
Plasma Plume
Clear Surface
Minimalized HAZ
No Melted Zone
No Microcracks
Large Concentration of Heat
Melted Zone
Heat Affected Zone (HAZ)
Liquid Phase
Microcracks
Heat Conduction to the Surrounding Material
Surface Distortions and Debris

## Slide 9: Experimental Setup
Set plate at angle Θ°
Run process
Gather data
Calculate Z offset
Correlate with hatch marks (and thermal data)
Fixture
Fixture
Fixture
Test Specimen
Beam
Θ
(Z) Focal Plane
Z + dz
Z - dz
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 10: Global Thermal Analysis
Intensities Relative
Able to define “athermal” ablation range
Helps make smart decisions for laser parameters
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 11: Confocal data: Sand to Black vs CLASP
Sand to Black
CLASP
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 12: Confocal data: Sand to Black vs CLASP
Sand to Black
CLASP
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 13: Tape PMC Emissions QA Study
Viewing emissions of the Carbon Fiber
  Can see where resin remains with higher contrast than visual
  Useful for fast closed loop feedback
Enables less damage and makes a more efficient process!
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 14: Closed Loop Processing
Taking data from the emissions, feed a dxf for the next pass
Reduces processing time up to 50% depending on number of passes
Homography required to correct for lens distortion
Emissions data filtered
DXF files with vectors in DMC software
1 Pass
2 Passes
3 Passes
4 Passes
5 Passes
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 15: CLASP Cart Timeline
Bench-top demonstration
CLASP Cart Rev 1
CLASP Cart Rev 2
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 16: CLASP Cart-Rev 3 April 2022
Enabling technologies
  20W Femtosecond Laser
  Up to 20m Hollow Core Fiber
Key Features
  Operator Safety interlocks
  Galvanometer based end effector
    6”x6”x6” focal range
  In-situ cameras
  HEPA processing exhaust
System Maturation
  System is deployed to a manufacturing facility
  Commercialization effort with Albers Aerospace in progress
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 17: Broadening Application Spaces
What are our customers asking for?
  More power/faster processing
    Targeting large area processing (50ft+)
      Robotic | Gantry Integration
  More fiber coupling options
    UV, higher power/energy capability, more flexible/durable
  Lighter weight
    Handheld processing / Small form factor lasers
New Areas of interest
  Coating removal (advanced coating systems, paint, etc…)
  Coating surface prep (ceramic/metal)
  Broad area surface functionalization
  Contamination remediation
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 18: Next Steps
Continued Advanced Integration
  Robotic
  Large Gantry
Improved Sensing
  Surface Mapping
  Custom emissions cameras
  Spectroscopy (LIPSS)
  Thermal
Diversify Applications Space
  Focusing in Aerospace
DISTRIBUTION STATEMENT A. Approved for public release: distribution unlimited. AFRL-2022-4992

## Slide 19: Questions?
Jimmy John
Laser Research Engineer | Laser Manufacturing Technology Development
Additive Manufacturing Technology Development Group
Structural Materials Division
James.John@udri.udayton.edu