## Slide 1
Application of Progressive Failure Analysis for Predicting Ultimate & Residual Strength of Composite Bonded Repairs
John Lin, Michael Fleming, Erick Espinar-Mick, The Boeing Company
Reewanshu Chadha, John Bakuckas, FAA Technical Center
June 16, 2023
@JCAMS

## Slide 2: Outline
Introduction
  Boeing-FAA Collaborative Research Agreement
  Regulatory Requirements for Composite Bonded Repair
Progressive Failure Analysis Fundamentals
  Composite Failure Theory & Models
  Adhesive Characterization & Modeling
  Automated Model Generation Tool
Application Cases
  Thermoset CFRP scarf repair with intact repair patch
  Thermoset CFRP scarf repair without repair patch
  Fiber oriented repair static strength
Conclusions & Future Work

## Slide 3: Introduction – Importance of Repair
China Airline Flight Cl611 In-Flight breakup over the Taiwan Strait, May 25, 2002
Boeing 747-200, B-18255
Cause:
  Tail strike (in Year 1980) damage in Section 46 was NOT removed (trimmed)
  Repair doubler did NOT extend sufficiently beyond the entire damaged area
  C/D Checks did not find cracks in 22 years
.063 2024-T3
Bolted doubler repair
Safety of Flight Depends on Proper Repair, Substantiation & Inspection
Ref: ASC-AOR-05-02-001

## Slide 4: FAA-Boeing CRADA 2007 – 2017: Bonded Repair on Metallic Structures
Joint FAA-Boeing FASTER Test Fixture
Well Designed & Executed Bonded Repair Can Suppress Crack Growth Rate to Zero

## Slide 5: Bonded Repairs to Primary Composite Panels 2018-Present
Bonded Repairs
Inspections
Testing & Analysis
Objective
  Study fatigue and residual strength performance of bonded repairs to representative composite structures
Tasks
  Assess damage tolerance capabilities and long-term airworthiness of bonded repairs
  Assess the ability of Structural Health Monitoring (SHM) and Non-Destructive Inspection (NDI) technologies to monitor repair integrity
  Verify and calibrate analysis methods used to analyze and design bonded repairs
Work Split
  FAA Tech Center: Test Fixture Design & Fab, Testing, NDI
  Boeing: Test Article Fab, Analysis, NDI Support, Post-Test inspection
  Publication: FAA & Boeing

## Slide 6: Airframe Beam Structural Test (ABST) Fixture Description
Fiberglass channels allows effective load transfer to wing skin test panel
Central Actuators (50 kip capacity), A1 and A2
End Actuators (50 kip capacity), A3 and A4
Wing skin test panel (24” x 40”)
Reaction structure
Loading Module
Wingbox Assembly
Carbon Fiber Reinforced Polymer (CFRP) Test Panel
Intentional Damage
Re-usable Steel/Fiberglass Substructure
Wingbox Assembly
Combined Tension/Compression & Shear Capability, Static & Fatigue (0.5 HZ)
Achievable Limit:
6,000 micro-strain
under tension for laminates up to 45 plies

## Slide 7: Regulatory Requirements for Composite Bonded Repair
Bonded repairs (Advantages)
  Desirable due to superior fit and finish
  Aerodynamically and structurally efficient
  Eliminates the region of high stress concentrations near the rivet holes
Bonded repairs (Challenges)
  Improve inspection methods to detect weak bonds that result in failure
  Repair processes are specialized and requires properly trained/qualified individuals
Major bonded repairs need to restore ultimate static strength (AC 25.1529-1A, AC20-107B)
  Fail-safety
  Damage Tolerance with Inspection
Critical structure (PSE for transport category) must have limit load strength capability in the case of failed repair for aircraft TC’ed after 11/24/2014 (PS-AIR-20-130-1)

## Slide 8: Generic Composite Bonded Repair
Parent Composite Structure/Substrate
Repair Patch (Doubler or Scarf)
Adhesive (Film, Paste, or Resin (wet-layup))
Circular Scarf Repair Example

## Slide 9: Hashin Failure Criteria – 6 Parameter Model
Fiber Strength XC, XT
Matrix Strength YC, YT
Shear Strength SL, ST
Energy-Based Damage Evolution

## Slide 10: Adhesive Modeling
Traction-Separation Cohesive Model
Ref. Lin & Duong, American Society for Composites (ASC) 28th Technical Conference Proceedings, 2013

## Slide 11: Automated Scarf Repair Modeling Tool
Adhesive Bondline
Implemented as an ABAQUS Plugin
Circular, Race-track
Full or Partial Depth
Single-sized or Double-Sided

## Slide 12: Static Strength Prediction with Intact Repair Patch

## Slide 13: Summary of Residual Strength Tests (without repair patch)
Chart: Panel #
| 2 | 3 | 5 | 4 | 6 | 7 | 8 | 9 | 10
 | 1 | 1.4412 | 1.4298 | 0.69295 | 0.72245 | 0.80705 | 0.81223 | 0.79453 | 0.84086
Partial-Depth Scarf (Panels 3, 5)
Full-Depth Scarf (Panels 4, 6)
Double-Sided Scarf (Panels 7, 8)
Double-Sided Scarf with Repair (Panels 9,10)
Open Hole (3”)
Static
Fatigue
Full Depth
Double-Sided Scarf
Patch
w/o Patch Patch
Static
Static
Static
Fatigue
Partial Depth (50%)
Static
Fatigue
[±45fabric/-45/90/45/0/-45/90/45/0]s
Open-hole
Typical CFRP Panels

## Slide 14: Failure Index Contour at the onset of 100% Predicted Critical Load for Full Scarf Panel = 11370 lbs
Matrix Tensile Failure Index
Fiber Tensile Failure Index

## Slide 15: Failure Index Contour at the onset of 100% Predicted Critical Load for Partial Scarf Panel = 20117 lbs
Matrix Tensile Failure Index
Fiber Tensile Failure Index

## Slide 16: Partial-Depth Scarf vs Double Side Scarf
Single-Sided Partial-Depth Scarf
(B) Double-Sided Scarf with One-side Repair
Prying Moment Induced by Eccentricity
 High peel stress in bondline

## Slide 17: Double-Sided Repair
One-side repair patch remaining

## Slide 18: Failure Mode Correlation
Double-sided scarf with partial repair

## Slide 19: Bondline Progressive Failure Animation
Double-sided scarf with partial repair

## Slide 20: Test Results
IS6
IS5, IS11

## Slide 21: Strain Gage Correlation (Gages 6, 5, 11)
IS6
IS5, IS11
100% Applied Strain = 12,500 me
Double-sided scarf with partial repair
fraction of applied far-field Strain

## Slide 22
Remove only overlap plies in the fiber direction
Results in ~40% reduction in the tapered area of the scarf
Being investigated by European aerospace companies/consortiums
Limited published work shows potential strength equivalence to conventional taper scarfs (joint coupon tests)
Use of automated material removal processes for reduced footprint
Reduces skill level needed to perform high quality scarf
Increases accuracy and speed of material removal
Automated Fiber-Oriented Repairs

## Slide 23
Automated Fiber Oriented repair testing
Demonstrate equivalency between fiber oriented scarf and traditional scarf - proof of concept
Panel 1
Panel 2
Panels 3 and 4
Taper Repair Geometry
Stepped Repair Geometry
Fiber-Oriented Repair Geometry
[±45fabric/-45/90/45/0/-45/90/45/0]s

## Slide 24: Stepped vs. Taper, Conventional vs Fiber-Oriented Repairs
Open-hole
Conventional Taper Repair Geometry
Stepped Repair Geometry
Fiber-Oriented Repair Geometry
Chart: Panels
| Open Hole | Tapered | Stepped | Fiber-Oriented | Fiber-Oriented (45s flipped)
Test | 1 | 1.3932 | 1.2589 | 1.2093 | 1.1996
Progressive Failure Analysis | 0.89324 | 1.4631 | 1.3927 | 1.238 | 1.238
Conclusion: Fiber-oriented repair is viable. It restores panel strength to120% of OHT

## Slide 25: Panel 2, Stepped Scarf with Repair: Failure Mode Comparison
OML Side
IML Side
Damage Sequence Predicted By PFA:
Bondline Failure  Fiber Breakage  Net-Section Panel Failure

## Slide 26: Conclusions and Future Work
Progressive failure analysis (PFA) correlated well with composite bonded repairs with or without repair patch.
With the aid from building block composite ply-level testing and adhesive testing, PFA can be utilized to enable smart testing. In applying Hashin failure criteria, be aware:
  Lamina level strength testing required
  Delamination not explicitly accounted for (can be incorporated albeit computationally expensive)
Future Work: Safety and Durability of Configured Composite Structural Repair
  152” x 60” , 5- stringer Test Panel Capability
  Shear, Bending and Torsion loading capability
  Up to 3,390,000 lbs anticipated load in the panel
  Based on typical wide body mid-span wing panel
  Sized for residual strength testing up to
  10,000 microstrain compression
  10,000 microstrain tension axially
  6,000 microstrain shear
  Fatigue spectrum test capability