## Slide 1: Army Composite Repair and Modification Procedure Guidelines
JCAMS Annual Meeting, Cape Canaveral FL
13 June 2023
FCDD-AMR-SF-M | Ranae Wright, SRD
Distribution Statement A. Approved for public release: distribution unlimited.

## Slide 2: Agenda
Background
Airworthiness
Material Manufacturer
Standardization
Technical Writing Guideline
Materials
Training
Facilities & Equipment
Path-forward
References

## Slide 3: BACKGROUND
Army composite rotor blades have been around for over 30 years but still has limited repair procedures and experience…
Fairing repairs are limited due to track and balance of blades
Blade spars are not allowed to be repaired
Limited training and experience on advanced composite repair processes
Tools and equipment for advanced composite repairs were not available
Lack of coordination between different systems and sub-systems (e.g., rotors, airframe, etc.)
Legacy manuals often contain outdated materials and processes which makes repairs longer to complete and lower quality
    Use of heat guns and lamps have large variability and unreliable
    Use of extended cure times due to room temperature cures
Comanche was intended to lead the way for Army airframe composite repair but was cancelled in 2004
Started upgrading carbon fiber repairs for stabilators in 2008
Notes: Background information for Army Composites
  Rotor blades have been around for over 30 years, but still have limited repair procedures and experience
  Fairing repairs are limited on blades – because blade require specific weight distribution for tracking and balance of the blade
  Army has limited training and experience on composite repair processes
    For example, tools and equipment
    Performing unauthorized repairs with unauthorized materials
  OEM/Maintainers often have a lack of coordination for composite repair procedures. Systems and sub-systems are segregated for example airframe vs rotors
  Legacy manuals had outdated materials and processes
    For example outdated procedures:
      Room temperature cure repairs (extended cure times)
      Use of heat guns or heat lamps (variability is unreliable)
      Temperature labels to are still being used in TM’s
      Jute felt (natural fiber) used as a breather cloth
  Comanche cancellation resulted in stopping advanced composite repair implementation
  In 2008, CF repairs were upgraded. For example: stabilator repairs

## Slide 4: Airworthiness of Composite repairs
  Factors that affect airworthiness:
  Fiber, tow size, and weave style
  Resin, mix ratio, shelf life, pot life, viscosity
  Number of plies, ply orientation, and ply overlap
  Fiber volume ratio, resin application, and bleed schedule
  Cure cycle – time, temperature, and pressure
  Training that is up-to-date, regulated, and recurring
  Surface prep and contamination control
  Facilities and environment
  Tools, equipment, and material availability
  Etc...
Bottom Line:
  EVERYTHING affects AIRWORTHINESS OF A COMPOSITE REPAIR!
Notes: There are many factors that can affect the airworthiness of a composite repair. Here are a few examples:
Fiber type, tow size, weave style (which we are all aware of)
Mix ratio (common issues)
Ply orientation and number of plies
How you apply resin
Using an accurate bleed schedule
Cure cycle – time, temperature, pressure
Everything affects airworthiness of a composite repair…for example, next slide

## Slide 5: Highlights
For composite repairs:
The technician performing the repair is the ‘Material Manufacturer’
Competence of the technician in the field, depot, or factory directly impacts the strength of the repair.
Notes: ***As it currently stands, all field repairs fall on the same soldier, every aircraft is maintained by the 15G MOS (military operation specialty)
Often times these repairs are not inspectable
Factory = Contractor Repairs and Modifications
Field = out in the field (e.g., desert)

## Slide 6: Standardization
We want it done right the first time, every time
MAINTAINING CONSISTENCY IS CRITICAL
Consistency across platforms, soldiers, training, tools/equipment, repair procedures and materials aids technical writers across various platforms…
  Expedites publication
  Reduces:
    probability of errors
    damaging the structure
    burden on maintainers
    likelihood of lower quality repairs
    logistics burden on the field and used across multiple platforms and parts
    cost
Notes: Giving information the correct way within the appropriate time to perform the work
Maintaining consistency is critical
  Consistency across
    Platforms
    Soldiers
    Training
    Tools/equipment
    Repair procedures
    Materials
  All help technical writers across various platforms
WHY?
  Expedites the publication process
  Reduces:
    Probability of errors (Soldiers on deployment will encounter and may be required to repair multiple aircrafts/vehicles (that they were not originally trained to maintain)
    Damaging the structure during repairs (Goes back to training and standard processes which will be covered in more detail later)
    Burden the on maintainers (consistency makes it easier to train technicians and lowers downtime on reworking repairs)
  Likelihood of lower quality repairs
    By moving towards elevated cure for both primary and secondary composites (reduce cost, time, and increase quality)
    Reduces the likelihood of a lower quality secondary structure repair process used on primary structure
  Reduces logistics burden on the field and across multiple platforms
  Cost
    Better aircraft availability
    More parts with better quality
    Standard repair materials reduces number of qualification tests
    Use of existing repair materials and tools

## Slide 7: Technical Writing guideline
Provides instructions and guidance on the development of New composite and adhesive bonded repair procedures with a more efficient and effective path toward airworthiness
Provide Army engineers clear guidelines for composite and adhesively bonded repairs and process modifications for fielded and future aircraft.
    Equipment/tooling
    Training
    Facilities
    Materials and processes
    Repair limits
Execute instructions with clear, consistent, and effective plans across all Army platforms.
Notes: There is an increase in the need for composites and adhesively bonded repairs in DOD applications

## Slide 8: Standard repair Guideline
EACH REPAIR PROCEDURE SHOULD LOOK/SMELL/FEEL/TASTE THE SAME ON A LEGACY AS A NEW PLATFORM
  May have different numbers of plies & ply orientations but all presented in the same format.
  Standard cure cycles for each material
  Standard set of bleeder materials. May use more layers of bleeder though.
  Maximize use of commercially available (SAE AMS specs, CMH-17 allowables) or government owned data
REPAIR GUIDELINES PAPER:
  Based on IETM MIL STD & experience on multiple IETM programs
  Different tech writers use different standards
  1st Priority – Unrepaired Damage Limits
  Standard WCNs
  Standard ply table format
  Standard part diagrams, bleeder diagrams, etc.
  No references to drawing
  Consolidated work packages
    Resin Mixing
    Wet layup
    Cure

## Slide 9: Guidelines Updates since 2016
Added:
    Resin Mix Ratio Tables from 25-100 g
    More on substantiation because RSIP was published 2018
    Section on Factory/Contractor Repairs and Modifications
    Material spec must be tied to a NSN (National Stock Number)
    Inspection maps to include details regarding substructure that could affect inspections
Updated:
    Requirements for cure cycle and bleed schedules
    Temperature ramp tolerances to ±3°F/min
    Requirement for process control sheets
    References
    Validation checklist
Notes: Our composite and adhesively bonded repair guidelines have made a few updates since 2016
25-100gram
  25g is the minimum mix ratio based on the scale in the Composite Shop Set (not going to have drastic errors in the mix ratio)
  100g is a good limit for maintainers when adding >100g of material (more often you are not going to have to mix more than 100g)
Temp. Ramp tolerances were too difficult to meet

## Slide 10: Materials
Standardizing the list of composite repair materials minimizes the number of materials, tools, and processes across parts and aircraft.
    Lowers the need to qualify & provision excessive repair materials
    Using consistent fiber to resin ratios across repair processes, for the same wet lay-up materials (i.e., SGP196P/EA9396 or 7781 fiberglass/EA9396)
Field Repairs:
  7781 & 120 fiberglass
  IM7, 6K plain weave carbon fabric (197 gsm)
  Epocast 1633/1652 potting compounds
  Adhesives:
    EA9394 paste adhesive
    EA9359.3NA or EA 9309.3NA paste adhesives
    EA9396 laminating resin
  All structural repairs need elevated temperature cure
Depot Repairs:
    Ability to use prepregs/film adhesive for lighter and larger repairs
      AMS 3970 repair materials
    New thicker components make wet layup repairs impractical
Notes: Mention paste adhesive viscosities - some would argue that 9309.3 is a low viscosity vs a high viscosity.
  We use EA9309.3 because of its low viscosity for forming nice core filets.
Also referenced AMS 3970 repair materials for depot. Can talk to their CMH-17 allowables & buying them by the yard from distributors.

## Slide 11: Training
training is everything
    Depot and field technicians need to be certified prior to working on advanced composite structure.
        Reduces errors for operating equipment/tools during the repair process
        Maximizes the strength of the repair
          Secondary structure processes should be equivalent to primary structure
        Reduces bad repairs
        Techniques are not provided in manuals
        Leveraging commercial aviation training resources
          SAE AIR 5719 and 4938
          FAA Advisory Circular, AC 65-33A
Notes: ****Leverage commercial aviation training as much as possible
Maintainers have limited training/experience on advanced composite repair processes
  FAA AC 20-107B Training for impact damage awareness – Cultural changes, must include impact damage awareness
  Existing FOD Training
  Management training – ABARIS courses
  Recurring Training – yearly up-to-date training
  2-210th (revised curriculum in June 2013) Up to 44 to 105 hours in Oct. 2016
  PIF training >250 15G Trained from 2-210th and field units
  Training/certification levels must be listed at the beginning of each applicable work package
  Technicians, both depot and field, need to be trained and/or certified prior to working on advanced composite structure
      For example, Double vacuum debulk (DVD) requires specific training and must be frequently done to retain proficiency
      Errors in operating ovens and autoclaves has resulted in quality escapements
      Repair training for secondary structures must be equivalent to primary structure to avoid confusion with maintainers.
      Consistency reduces the likelihood of a lower quality secondary structure repair process used on primary structure
    Reducing technical detail in each DMWR work package due to requirements in training/cert requirements. These training/cert. covers functions such as paint removal, damage removal and layout, Impregnation, vacuum bagging, cure process management, and inspection
      Upgrade CCAD training requirements. Proposed breakout includes
          Apprentice: Wet lay-up on secondary structure
          Journeyman: Prepreg/DVD repairs on highly loaded critical structure
          Advanced: Capable of rebuilding aircraft components
SAE AIR 4938 Rev. C, Composite and Bonded Structure Technician/Specialist Training Document , dated 2018.
  Composite and Bonded Structure Technician/Specialist Training Document
SAE AIR 5719 Rev. A, Teaching Points for a Class on ‘Critical Issues in Composite Maintenance, Repairs, and Overhaul’, dated 2018
  A standard teaching checklist for a course covering the critical technical issues associated with the maintenance, repair, and overhaul of composite aircraft structures.

## Slide 12: Facilities and equipment
Field Repair
  Limited facilities and hangars
    Wet layup/hot bonder repairs
  No controlled storage/environment
Depot Facilities
  Must be equivalent to OEM facilities
  Elevated temperature cures
  Prepreg and film adhesive materials require cleanrooms to layup patches
  Consideration for minimizing unique types of tools, materials, and expendable items
Tools and Expendable Items
  Field repairs
    Limited to Composite Shop Set
    All battle damage shall use the tools and expendable items from BDAR Kit unless substantiation is provided
  Depot repairs
    Not limited to the Composite Shop Set but should start with the shop set tools
Notes: ***Everything mentioned in the -11 (tools and equipment) are not fielded*** (Example, DVD tooling)
Battle Damage Assessment and Repairs (BDAR)
  Must be portable
  No power to operate hot bonder
N10 Breather call-outs for autoclaves not in repair (N4 is fielded)
TASMG, contract maintenance can make their own clean rooms to improve productions but its not required for the field environment.
Either a hot bonder/heat blanket or an oven can be used to cure adhesives
Repair procedures need to specify the exact tools for damage removal and machining.
  Drill reamers are not appropriate for drilling a single facesheet on thin sandwich structures. The full diameter of the bit will not be reached before the bit penetrates the far side or opposite facesheet.
Intermediate, sub-sets of the shop-set. All the tools start with the composite shop set
Damage limits and repair sizes need to consider the impact of repairing the component in an uncontrolled field environment
Should reference a Commercial Item Description (CID) or industrial specification.
  Eliminates specifying a particular manufacturer
  Provides flexibility to the depot to make cost effective procurement
Additional Notes:
Some repairs may require Depot level repair depending on what it is.
Production facilities often already have a facilities specification.
Factory repairs still require substantiation and damage limits for repaired and unrepaired damage must be specified.
Air force repair facility guidance

## Slide 13: Path-Forward
Composites repairs need to be addressed early on in a program. For example:
  Damage limits
  Repair substantiation
  Materials
  Tools/equipment
  Facilities
  Training
Benefits of Standardization:
  Utilizing the same materials, tools, and processes across platforms
  Lowers cost overall
  Lowers additional costs for composite training requirements and processes
  Reduces burden on maintainers
Will continue to leverage repair resources across DoD
  TM 1-1500-204-23-11
  Air Force T.O. 1-1-690
  NAVAIR 01-1A-21
Notes: ***Guideline is not a recap of TM 1-1500-204-23-11 but a resource that includes best practices and recommendations for repairs and modification manuals from lessons learned over the past 30 years. This guideline is a working document that will improve as new materials, platforms, and training develop and change over time.
Current manuals have updated procedures for carbon repairs across multiple platforms

## Slide 14: References
TM 1-1500-204-23-11, Change 0, Advanced Composite Material General Maintenance and Practices
Air Force T.O. 1-1-690, Technical Manual General Advanced Composite Repair Processes Manual
NAVAIR 01-1A-21, Technical Manual Organizational And Intermediate Maintenance General Composite Repair
SAE AIR 4938 Rev C, Composite and Bonded Structure Technician/Specialist Training Document
SAE AIR 5719 Rev A, Teaching Points for a Class on ‘Critical Issues in Composite Maintenance, Repairs, and Overhaul’
MIL-STD-3063, Rotorcraft Structural Integrity Program
MIL-STD-40051-1B, Preparation Of Digital Technical Information For Interactive Electronic Technical Manuals (IETMs)
MIL-STD-40051-2B, Preparation Of Digital Technical Information For Page-Based Technical Manuals (TMs)
MIL-HDBK-17F, soon to become CMH-17G
FAA Advisory Circular AC 20-107B, Composite Aircraft Structure
FAA AR 03/19, Material Qualification and Equivalency for Polymer Matrix Composite Material Systems
FAA AR 08/54, Guidelines for the Development of a Critical Composite Maintenance and Repair Issues Awareness Course
FAA AR 09/3, Online Course and Regional Laboratory Development in Composite Maintenance Education, Including Training Repair Manual
FAA Advisory Circular, AC 65-33A, Subject: Development of Training/Qualification Programs for Composite Maintenance Technicians
FAA Advisory Circular, AC 145-6, Repair Stations for Composite and Bonded Aircraft Structure
Introduction To Establishing Air Force Clean Facilities For Composite Processing, USAF Advanced Composites Office, Hill AFB, Utah
Air Force Advanced Composite Facility Guide, USAF Advanced Composites Office
SS8888, Composite Components, General Process Specification for
BAC5317, Fiber Reinforced Composite Parts
HP 17-0, Clean Room, Environmentally Controlled, Requirements For
JTDI website includes composite resources page -https://www.jtdi.mil

## Slide 15
CONTACT INFORMATION:
Dave Stone
Lead Engineer, Non-Metallic Materials
Army DEVCOM Aviation & Missile Center
Redstone Arsenal, Alabama
J. Ranae Wright
Materials Engineer
Army DEVCOM Aviation & Missile Center
Redstone Arsenal, Alabama